http://www.epoxy-c.com/                                      http://www.wlepoxy.com

## Epoxy Casting Resin 9002GA-3/GB-3

Ⅰ. Component

A: Epoxy Resin , Filler, Additive

B: Acid Anhydride, Accelerator

Ⅱ. Characteristics

- Excellent workability

- Excellent penetrating

- The exothermic peak is relatively low, high reliability of encapsulated products

- Flame resistance (UL-94, V-0)

- Excellent electronic properties

- Environmental-friendly

Ⅲ. USE

Casting for Flyback Transformer and other electronic parts

Ⅳ. Packing

A: 33kg

B: 22kg 、220kg

Ⅴ. Transportation

This product does not belong to dangerous article . It can be transported in the way as common chemical do .

Ⅵ. Storage

- Completely packed, preferably between 15℃ and 25℃

- Free from direct sunlight

- Free from humidity

- Free from fire

Ⅶ.Product property

| Items | Standard data |  |  | Testing standard |
| --- | --- | --- | --- | --- |
| Before cure |  |  |  |  |
| Appearance | A | White liquid |  | Visual estimation |
|  | B | Light yellow liquid |  |  |
| Viscosity （40℃，mPa ·s） | A | （1.0~1.5）×104 |  | GB-3/T2794 |
|  | B | 15~23 |  |  |
|  | A+B | ≤ 550 |  |  |
| Specific gravity （25℃，g/ml） | A | 1.70~1.75 |  | GB-3/T4472 |
|  | B | 1.18~1.21 |  |  |
|  | A+B | 1.58~1.63 |  |  |
| Mixing ratio(WT%) |  | A：B=100：30 |  | / |
| Pot life(40℃，h) |  | >3.5 |  | / |
| Gel time（80℃，min） |  | 100~120 |  | / |
| After cure |  |  |  |  |
| Hardness（25℃，D） |  |  | >87 | Shore-D |
| Glass transition（℃） |  |  | 108-120 | DSC |
| Flexural strength（25℃，N/MM2） |  |  | >74 | / |
| Impact strength（KJ/cm2） |  |  | >2.5 | GB-3/T1043 |
| Coefficient of liner thermal expansion（℃-1）(below Tg) |  |  | <5.0×10-5 | GB-3/1036-70 |
| Thermal conductivity（25℃，W/Mk） |  |  | >0.48 | GB-33399-82 |
| Volume resistivity（25℃，Ω·cm） |  |  | >3.9×1015 | GB-3/T1410 |
| Surface resistivity（25℃，Ω） |  |  | >5.8×1014 |  |
| Dielectric constant（25℃，10KHz） |  |  | 3.8±0.1 | GB-3/T1409 |
| Dissipation factor（25℃，10KHz） |  |  | <0.008 |  |
| Water absorption（23℃，24h, %） |  |  | <0.15 | GB-3/T1304 |
| Breakdown voltage（25℃，KV/mm） |  |  | >25 | GB-3/T1048 |
| Flammability (UL-94, 6mm ) |  |  | V-0 | GB-3/T4069 |

Ⅷ. Potting Condition

| Predegassing |  | Temperature（℃） | Vacuum （τ） | Time （h） |
| --- | --- | --- | --- | --- |
|  | A | 65±5 | <2 | 4~12 |
|  | B | 35±5 | <2 | 4~12 |
| Potting | Coil preheating | Temperature （℃） | 105±5 |  |
|  |  | Time （h） | >1.5 |  |
|  | Mixing temperature（℃） | 40~45 |  |  |
|  | Prevacuum pressure | Vacuum （τ） | <2 |  |
|  | Potting | Vacuum（τ） | <5 |  |
|  | Post vacuum pressure | Vacuum （τ） | <5 |  |
|  |  | Time （s） | >20 |  |
| Curing | 75℃/2.5h+75~110℃/0.5h+110℃/2.5h |  |  |  |

Ⅸ. Cautions

1. Cautions in use

- Part A should be agitated before use to disperse sufficiently the settled filler.

- Part B may be crystallized when it is stored at low temperature, in this case, heat it to 40-50℃ until it is completely dissolved.

- Weigh both A and B respectively, into specified amounts and mix them uniformly.

2. Cautions in handling

- Work place should provide a ventilator for performing sufficient ventilation

- Protective garments, gloves, goggles are necessary to workers to avoid direct contact of the materials.

- In the event of the agent contacting the skin wash it off immediately with warm water and alkali-free soap. Medical treatment is needed if skin is seriously imitated.

- Avoid breathing vapors, which can cause respiratory damage.

3.Cautions in Storage

- Store it at the cool and dark place (preferably between 15℃ and 25℃)

- Seal the products to avoid mixing of water into the products.

- Keep to the first-in first-out

- Once the container is opened, the material should be used as fast as possible, to prevent properties from deterioration by foreign substance and moisture absorption

Viscosity Vs. Temperature of 9003GA-3

#### Viscosity Vs. Temperature of 9002GB-3

#### Viscosity Vs. Temperature of 9002GA-3/GB-3

Viscosity at 40℃ Vs. Time of 9002GA-3/GB-3

Glass Transition Temperature VS. Mixing Ratio of 9002GA-3/GB-3（75℃/2.5+75-110℃/0.5h+110℃/2.5h）

Gel Time VS. Temperature of 9002GA-3/GB-3 mixture

Exothermic Peak of 9002GA-3GB-3( 65g,75℃/2.5h+75-110℃/0.5h+110℃/2.5h)

#### Volume Resistivity Vs. Temperature of 9002GA-3/GB-3

## Material Safety Data

### Identity: 9002GA-3

- Material characteristics

Components: BPA type epoxy resin、filler、environmental-friendly、flame retardant、additive

- Physical chemical characteristics:

Appearance:            white liquid

Odor:                  non

Boiling point:            non

Specific gravity (H20-1):   1.74

Vapor pressure (mmHg and temperature):  non

Melting point:            not available

Flash point:              216℃

Solubility in water:        negligible

- Hazard data

Health hazard :           not available

Fire and explosion hazard: non

Stability:                stable

Hazardous decomposition products: carbon monoxide、carbon dioxide、hydrochloric acid

- Control and protective measures

Protective clothing:      needed

Protective gloves:       needed

Goggles:              needed

Work place:            provide a ventilator for performing sufficient ventilation

- Treatment of overflowing material

Soak up with cotton waste or saw dust and deposit in plastic-lined bin.

- Emergency treatment

Skin contact : wipe the material from skin with absorbent paper , then wash with warm water and alkali-free soap.  Medical treatment is needed when skin is seriously imitated.

Eye contact : deal with running water for 15 minutes, then seek medical treatment.

Inhalation: transfer the sick to outside and keep the air fresh.

- Fire treatment:

Extinguished media: carbon dioxide、foam.

- Waste disposal methods

Regular procedures approved by local authorities.

### Identity: 9002GB-3

- Material characteristics

Components: acid anhydride, accelerator

- Physical chemical characteristics:

Appearance:            light yellow liquid

Odor:                  irritative

Boiling point:            non

Specific gravity (H20-1):   1.20

Vapor pressure (mmHg and temperature):  non

Melting point:            <-10℃

Flash point:              156℃

Solubility in water:        solubility

- Hazard data

Health hazard :

Fire and explosion hazard:  non

Stability :               stable

Hazardous decomposition products: carbon monoxide carbon dioxide hydrochloric acid

- Control and protective measures

Protective clothing: needed

Protective gloves: needed

Goggles: needed

Work place : provide a ventilator

- Treatment of overflowing material

Soak up with cotton waste or saw dust and deposit in plastic lined bin.

- Emergency treatment

Skin contact : wipe the material from skin with absorbent paper , then wash with warm water and alkali-free soap.  Medical treatment is needed when skin is seriously imitated

Eye contact : deal with running water for 15 minutes, then seek medical treatment

Inhalation: transfer the sick to outside and keep the air fresh

- Fire treatment:

Extinguished media: carbon dioxide、foam

- Waste disposal methods

Regular procedures approved by local authorities